|  | # Wire Technology, Process Engineering and Metallurgy Roger N. Wright Butterworth-Heinemann |
| --- | --- |

This document is overwritten when you make changes in Play Books. You should make a copy of this document before you edit it.

# Annotations by color

# 18 yellow notes • 19 green notes • 18 blue notes • 11 red notes

Created by David Kirchner   – Last synced November 24, 2023

## Yellow

exerted Force = Pounds = Newtons = Kg*9.8 mass*gravity Work and energy = foot-Pounds = Newton Meters Power = Horsepower = Foot-Pounds/Seconds = watts hp =550 Ft*Lb/sec = 746 watt Stress = Force/Area = psi = pascal = Newton/Sq Meter 1 ksi = 6.894 MPa Tensile Strain = (lf-lo)/lo September 3, 2023; 37.

Strain Rate strain rate = speed / length of deformation zone September 3, 2023; 39.

ow ▵ values are associated with low die angles and high reductions, and high Δ values are associated with high die angles and low reductions. September 4, 2023; 42.

Centerline tension in drawing is of great concern because it promotes the development and growth of porosity and ductile fracture of the wire at the centerline. Moreover, it inhibits the stabilization and densification of porous centerline structure inherited from casting operations. Fractures developing at the centerline during drawing are called “center bursts,” “central bursts,” and “cuppy cores.” September 4, 2023; 55.

In summary, deformation heating in a given pass does not depend on drawing speed unless there is a significant effect of strain rate on flow stress. Similarly, equilibrated frictional heating (downstream) from a given pass does not depend on drawing speed. October 8, 2023; 78.

drawing speed generally has a direct effect on lubricant film thickness and the related coefficient of friction October 8, 2023; 79.

For a given drawing lubricant, there may be a critical speed range at which hydrodynamic conditions are achieved. Or, for a given drawing speed, a critical viscosity range may be necessary, reflecting the chemical formulation of the lubricant and/or its temperature. October 8, 2023; 87.

Lubrication can be greatly impacted by the conditions of the incoming wire or wire surface, particularly when the wire or “redraw rod” has just been annealed or hot worked. In such cases, vigorous procedures (“pickling,” chemical descaling, mechanical descaling, shaving, scalping, etc.) may be employed to remove oxide and surface roughness. These procedures may leave surface quality that must be considered when lubrication is subsequently used in the drawing process. October 11, 2023; 94.

It must be emphasized that small reductions (increased ∆) are associated with increased die pressure. The phenomenon is well documented, however, and increased die wear is observed with light passes. October 11, 2023; 110.

Yet another manifestation of low ∆ die design and uniform metal flow is the absence or reduction of hydrostatic tension at the wire center. Such hydrostatic tensile stress has been shown to lead to porosity and central bursts at the wire center. October 11, 2023; 111.

9.5 CofF ave .08 to .12 for WC November 18, 2023; 117.

The ratio of draw stress to yielding/breaking stress reflects the work hardening that may take place in going through the die. November 18, 2023; 125.

High ∆ drawing, leading to greater degrees of redundant work and a greater potential for nonuniformity. October 11, 2023; 130.

• Worn dies, since wear and the related interference with lubrication may not be circumferentially uniform.• Die misalignment, including intentional misalignments to create cast.• Misalignments of the “wire route” with the die holder (influences of capstans, guides, etc.).• Dies drilled off center, or with asymmetric blends.• Vibrations along the wire route. October 11, 2023; 130.

n many cases, however, the individual grains are not randomly oriented, and many grains will be oriented close to a preferred grain orientation. Such a material is said to have a texture. A highly preferred grain orientation, or a “sharp” or “strong” texture, will have properties approaching those of a single crystal and can have rather anisotropic physical properties. October 11, 2023; 159.

planes with normals in the directions of the cube diagonals. November 24, 2023; 159.

Anything that interferes with dislocation motion will make slip more difficult and increase the strength of the crystal. November 24, 2023; 160.

Cockcroft and Latham material constant, c, is a fundamental index of workability and drawability. October 12, 2023; 179.

## Green

In the lower Δ range, lighter reductions result in increased values of die pressure over and above the role of smaller reductions in increasing Δ November 18, 2023; 53.

Martensite is a phase that forms when certain alloys are cooled through and below a critical temperature. Concurrent stress and plastic deformation can affect the martensitic transformation temperatures. Thus the drawing temperature of such alloys can greatly affect drawn properties. This is the case for stock subjected to forming, bending, and torsion, such as in spring and fastener making. Common alloys displaying this sensitivity are austenitic stainless steels and shape memory alloys. October 1, 2023; 74.

The primary motivation for increased drawing speed is no doubt that of increased productivity October 18, 2023; 80.

Coefficient of friction values of, say, 0.15 are often used to represent conditions of local sticking. November 18, 2023; 86.

A reasonable protocol for high friction drawing involves the following guidelines:a. Draw stress minimizationb. Avoidance of Δ values much above threec. Avoidance of σd/σa ratios above 0.7 November 18, 2023; 94.

Die wear will generally be increased by increased die pressure, as caused by lighter reductions, higher die angles, higher ∆ values, and higher wire flow stress. November 18, 2023; 123.

The simplest pass schedule concept is constant area reduction, r November 18, 2023; 124.

The principle motivation for maintaining constant ∆ is to maintain reasonably consistent drawing mechanics, such as consistent values of die pressure, redundant work, and centerline tension. November 18, 2023; 124.

Wire often assumes a helical configuration, going onto spools or into containers, and may exhibit a helical configuration coming off of spools or out of containers. Assuming the helical configuration has a longitudinal axis, t November 23, 2023; 128.

the cast is described by the radius of curvature about that axis, and the pitch is the advance of the wire along that axis in one revolution. November 18, 2023; 128.

cast and pitch control have been attempted by alignment or controlled misalignment of the finishing die November 18, 2023; 129.

Drawing or pulling the workpiece through rollers to effect a change in cross-sectional area or shape differs from simple drawing in that very little friction is created by the rollers, and a lubricant may not be necessary November 24, 2023; 138.

The total energy per unit volume en route to fracture is called toughness. November 23, 2023; 157.

As plastic strain accumulates, the number of dislocations begins to multiply and the total length of dislocations per unit volume of crystal begins to increase. This increase in dislocation density leads to a certain congestion in dislocation motion; that is, pileups and tangles of dislocations occur that increase the stress required for continued dislocation motion (and slip) November 24, 2023; 160.

deformation twinning is usually only seen when slip is difficult. November 24, 2023; 162.

predictor of drawability, ln(A0/Af) November 24, 2023; 179.

In the simplest concept of drawing, a break occurs when the draw stress equals the yield and/or breaking stress of the wire at the die exit November 24, 2023; 185.

During most drawing operations, the surface of the wire undergoes “wear” (wire wear as opposed to die wear), and small pieces of the wire (called “fines”) flake off November 24, 2023; 190.

The resistance of stainless steels to corrosion arises from the tightly adhering, relatively impervious chromium-oxygen layer that forms on the alloy surface. November 24, 2023; 257.

## Blue

with effective temperature control it may be practical to draw at very high speeds (5000 m/min) October 18, 2023; 80.

pon start-up the wire speed increases from zero and usually traverses a speed range well below that of the intended steady state. In this range the lubricant may not be adequate, November 18, 2023; 80.

The wire may stick to the die and the dies may even be damaged. Such conditions are also pertinent to the very slow drawing speeds involved with die string-up. November 18, 2023; 80.

oxalates for stainless steel drawing November 18, 2023; 96.

Deformation zone shape is characterized by ∆, and ∆ is a function of reduction and die angle. November 18, 2023; 108.

wire abrasion at the die entry in the event of die misalignment. This is particularly important if the die is intentionally misaligned as a means of controlling or imparting cast in the as-drawn wire November 18, 2023; 118.

Relatively sharp blends are recommended for the drawing of high carbon steel and stainless stee November 18, 2023; 119.

Pressure dies offer an efficient way to greatly enhance lubricant pressure at the die entry without the requirement of nearly ideal lubrication or high drawing speed November 18, 2023; 121.

Archard equation, is widely used for general analysis of wear behavior November 18, 2023; 122.

Pass schedules designed for maximum reduction in each pass should involve a constant ratio of draw stress to yielding/breaking stress, since that ratio most directly represents the risk of breakage in ostensibly sound rod or wire. It is generally advisable that this ratio be below 0.7, and a value of 0.6 probably represents a practical maximum for an aggressive reduction schedule. November 18, 2023; 125.

for adiabatic conditions the temperature increase is proportional to the drawing stress. November 18, 2023; 126.

A pass schedule involving a steady decrease in per-pass reduction to offset work hardening is called a “tapered” pass schedule. November 18, 2023; 126.

Plane strain occurs where there is no spreading or increase in rectangular rod width during the drawing of the rod through the rolls November 24, 2023; 138.

strip width is ten times November 24, 2023; 138.

Roll Force Analysis for Plane Strain Rolling November 24, 2023; 140.

plastic flow involve crystallographic slip by way of dislocation motion. Hardness tests measure the resistance of material to an indenter, and hardness correlates well with flow stress. November 23, 2023; 145.

If a cold-worked structure is heated to above six-tenths of the melting point, the dislocation pileups and tangles are rapidly eliminated through increased thermal vibrations of the atoms. This occurs through the processes of recovery and recrystallization. November 23, 2023; 161.

Rockwell, Brinell, Vickers, Knoop, and variations within these tests. In general, these tests measure the resistance of the metal to an indenter. November 24, 2023; 163.

## Red

mean normal stress at the centerline October 6, 2023; 43.

The average stress at the centerline is less compressive than at the die wall and may even be tensile. This is particularly the case for higher values of Δ. September 4, 2023; 54.

In addition to increasing overall drawing stress and lowering die pressure and related friction, back tension adds directly to the value of centerline tension increasing the risk of fracture at the wire center September 4, 2023; 57.

through two dies in tandem, and the draw stress for the initial die constitutes a back stress for the final die October 17, 2023; 58.

a 100 °C increase in lubricant temperature can be associated with viscosity decreases of nearly two orders of magnitude November 18, 2023; 92.

the wire surface temperature may actually decrease somewhat with increased drawing speed, concurrent with an increase in lubricant temperature. November 18, 2023; 92.

die designs involving low ∆ values (i.e., low approach angles and/or large reductions) should offer superior performance in terms of reduced wear, reduced requirements for intermediate annealing, reduced cuppy core breakage, improved final product ductility, and minimization of thinning beyond the die exit. November 18, 2023; 108.

The redundant work contributes extra strain hardening, particularly at the wire surface, and limits the number of passes and overall reduction that can be taken before annealing is necessary. Thus, low ∆ die design should be consistent with reduced requirements for intermediate annealing. November 18, 2023; 111.

It also appears to react with carbide-forming elements such as iron, thus limiting its use in ferrous drawing November 18, 2023; 116.

11.3.2 Slip, Dislocations, and Plastic Flow in Crystals November 23, 2023; 159.

The slip occurs at a relatively low value of shear stress because the dislocation motion involves the rearrangement of a relatively small number of atoms at a time. November 24, 2023; 159.

# All your annotations

# 66 notes/highlights • 1 bookmark

## Chapter 4: Basic Engineering Variables Pertinent to Drawing

exerted Force = Pounds = Newtons = Kg*9.8 mass*gravity Work and energy = foot-Pounds = Newton Meters Power = Horsepower = Foot-Pounds/Seconds = watts hp =550 Ft*Lb/sec = 746 watt Stress = Force/Area = psi = pascal = Newton/Sq Meter 1 ksi = 6.894 MPa Tensile Strain = (lf-lo)/lo September 3, 2023; 37.

Strain Rate strain rate = speed / length of deformation zone September 3, 2023; 39.

ow ▵ values are associated with low die angles and high reductions, and high Δ values are associated with high die angles and low reductions. September 4, 2023; 42.

mean normal stress at the centerline October 6, 2023; 43.

## Chapter 5: Basic Drawing Mechanics

In the lower Δ range, lighter reductions result in increased values of die pressure over and above the role of smaller reductions in increasing Δ November 18, 2023; 53.

The average stress at the centerline is less compressive than at the die wall and may even be tensile. This is particularly the case for higher values of Δ. September 4, 2023; 54.

Centerline tension in drawing is of great concern because it promotes the development and growth of porosity and ductile fracture of the wire at the centerline. Moreover, it inhibits the stabilization and densification of porous centerline structure inherited from casting operations. Fractures developing at the centerline during drawing are called “center bursts,” “central bursts,” and “cuppy cores.” September 4, 2023; 55.

In addition to increasing overall drawing stress and lowering die pressure and related friction, back tension adds directly to the value of centerline tension increasing the risk of fracture at the wire center September 4, 2023; 57.

through two dies in tandem, and the draw stress for the initial die constitutes a back stress for the final die October 17, 2023; 58.

## Chapter 6: Drawing Temperature

Martensite is a phase that forms when certain alloys are cooled through and below a critical temperature. Concurrent stress and plastic deformation can affect the martensitic transformation temperatures. Thus the drawing temperature of such alloys can greatly affect drawn properties. This is the case for stock subjected to forming, bending, and torsion, such as in spring and fastener making. Common alloys displaying this sensitivity are austenitic stainless steels and shape memory alloys. October 1, 2023; 74.

October 1, 2023; 75.

## Chapter 7: Drawing Speed

In summary, deformation heating in a given pass does not depend on drawing speed unless there is a significant effect of strain rate on flow stress. Similarly, equilibrated frictional heating (downstream) from a given pass does not depend on drawing speed. October 8, 2023; 78.

drawing speed generally has a direct effect on lubricant film thickness and the related coefficient of friction October 8, 2023; 79.

The primary motivation for increased drawing speed is no doubt that of increased productivity October 18, 2023; 80.

with effective temperature control it may be practical to draw at very high speeds (5000 m/min) October 18, 2023; 80.

pon start-up the wire speed increases from zero and usually traverses a speed range well below that of the intended steady state. In this range the lubricant may not be adequate, November 18, 2023; 80.

The wire may stick to the die and the dies may even be damaged. Such conditions are also pertinent to the very slow drawing speeds involved with die string-up. November 18, 2023; 80.

## Chapter 8: Friction, Lubrication, and Surface Quality

Coefficient of friction values of, say, 0.15 are often used to represent conditions of local sticking. November 18, 2023; 86.

For a given drawing lubricant, there may be a critical speed range at which hydrodynamic conditions are achieved. Or, for a given drawing speed, a critical viscosity range may be necessary, reflecting the chemical formulation of the lubricant and/or its temperature. October 8, 2023; 87.

a 100 °C increase in lubricant temperature can be associated with viscosity decreases of nearly two orders of magnitude November 18, 2023; 92.

the wire surface temperature may actually decrease somewhat with increased drawing speed, concurrent with an increase in lubricant temperature. November 18, 2023; 92.

A reasonable protocol for high friction drawing involves the following guidelines:a. Draw stress minimizationb. Avoidance of Δ values much above threec. Avoidance of σd/σa ratios above 0.7 November 18, 2023; 94.

Lubrication can be greatly impacted by the conditions of the incoming wire or wire surface, particularly when the wire or “redraw rod” has just been annealed or hot worked. In such cases, vigorous procedures (“pickling,” chemical descaling, mechanical descaling, shaving, scalping, etc.) may be employed to remove oxide and surface roughness. These procedures may leave surface quality that must be considered when lubrication is subsequently used in the drawing process. October 11, 2023; 94.

oxalates for stainless steel drawing November 18, 2023; 96.

## Chapter 9: Drawing Die and Pass Schedule Design

Deformation zone shape is characterized by ∆, and ∆ is a function of reduction and die angle. November 18, 2023; 108.

die designs involving low ∆ values (i.e., low approach angles and/or large reductions) should offer superior performance in terms of reduced wear, reduced requirements for intermediate annealing, reduced cuppy core breakage, improved final product ductility, and minimization of thinning beyond the die exit. November 18, 2023; 108.

It must be emphasized that small reductions (increased ∆) are associated with increased die pressure. The phenomenon is well documented, however, and increased die wear is observed with light passes. October 11, 2023; 110.

The redundant work contributes extra strain hardening, particularly at the wire surface, and limits the number of passes and overall reduction that can be taken before annealing is necessary. Thus, low ∆ die design should be consistent with reduced requirements for intermediate annealing. November 18, 2023; 111.

Yet another manifestation of low ∆ die design and uniform metal flow is the absence or reduction of hydrostatic tension at the wire center. Such hydrostatic tensile stress has been shown to lead to porosity and central bursts at the wire center. October 11, 2023; 111.

It also appears to react with carbide-forming elements such as iron, thus limiting its use in ferrous drawing November 18, 2023; 116.

9.5 CofF ave .08 to .12 for WC November 18, 2023; 117.

wire abrasion at the die entry in the event of die misalignment. This is particularly important if the die is intentionally misaligned as a means of controlling or imparting cast in the as-drawn wire November 18, 2023; 118.

Relatively sharp blends are recommended for the drawing of high carbon steel and stainless stee November 18, 2023; 119.

Pressure dies offer an efficient way to greatly enhance lubricant pressure at the die entry without the requirement of nearly ideal lubrication or high drawing speed November 18, 2023; 121.

Archard equation, is widely used for general analysis of wear behavior November 18, 2023; 122.

Die wear will generally be increased by increased die pressure, as caused by lighter reductions, higher die angles, higher ∆ values, and higher wire flow stress. November 18, 2023; 123.

The simplest pass schedule concept is constant area reduction, r November 18, 2023; 124.

The principle motivation for maintaining constant ∆ is to maintain reasonably consistent drawing mechanics, such as consistent values of die pressure, redundant work, and centerline tension. November 18, 2023; 124.

Pass schedules designed for maximum reduction in each pass should involve a constant ratio of draw stress to yielding/breaking stress, since that ratio most directly represents the risk of breakage in ostensibly sound rod or wire. It is generally advisable that this ratio be below 0.7, and a value of 0.6 probably represents a practical maximum for an aggressive reduction schedule. November 18, 2023; 125.

The ratio of draw stress to yielding/breaking stress reflects the work hardening that may take place in going through the die. November 18, 2023; 125.

for adiabatic conditions the temperature increase is proportional to the drawing stress. November 18, 2023; 126.

A pass schedule involving a steady decrease in per-pass reduction to offset work hardening is called a “tapered” pass schedule. November 18, 2023; 126.

Wire often assumes a helical configuration, going onto spools or into containers, and may exhibit a helical configuration coming off of spools or out of containers. Assuming the helical configuration has a longitudinal axis, t November 23, 2023; 128.

the cast is described by the radius of curvature about that axis, and the pitch is the advance of the wire along that axis in one revolution. November 18, 2023; 128.

cast and pitch control have been attempted by alignment or controlled misalignment of the finishing die November 18, 2023; 129.

High ∆ drawing, leading to greater degrees of redundant work and a greater potential for nonuniformity. October 11, 2023; 130.

• Worn dies, since wear and the related interference with lubrication may not be circumferentially uniform.• Die misalignment, including intentional misalignments to create cast.• Misalignments of the “wire route” with the die holder (influences of capstans, guides, etc.).• Dies drilled off center, or with asymmetric blends.• Vibrations along the wire route. October 11, 2023; 130.

## Chapter 10: Shaped Dies and Roller Dies

Drawing or pulling the workpiece through rollers to effect a change in cross-sectional area or shape differs from simple drawing in that very little friction is created by the rollers, and a lubricant may not be necessary November 24, 2023; 138.

Plane strain occurs where there is no spreading or increase in rectangular rod width during the drawing of the rod through the rolls November 24, 2023; 138.

strip width is ten times November 24, 2023; 138.

Roll Force Analysis for Plane Strain Rolling November 24, 2023; 140.

## Chapter 11: Mechanical Properties of Wire and Related Testing

plastic flow involve crystallographic slip by way of dislocation motion. Hardness tests measure the resistance of material to an indenter, and hardness correlates well with flow stress. November 23, 2023; 145.

The total energy per unit volume en route to fracture is called toughness. November 23, 2023; 157.

n many cases, however, the individual grains are not randomly oriented, and many grains will be oriented close to a preferred grain orientation. Such a material is said to have a texture. A highly preferred grain orientation, or a “sharp” or “strong” texture, will have properties approaching those of a single crystal and can have rather anisotropic physical properties. October 11, 2023; 159.

11.3.2 Slip, Dislocations, and Plastic Flow in Crystals November 23, 2023; 159.

planes with normals in the directions of the cube diagonals. November 24, 2023; 159.

The slip occurs at a relatively low value of shear stress because the dislocation motion involves the rearrangement of a relatively small number of atoms at a time. November 24, 2023; 159.

Anything that interferes with dislocation motion will make slip more difficult and increase the strength of the crystal. November 24, 2023; 160.

As plastic strain accumulates, the number of dislocations begins to multiply and the total length of dislocations per unit volume of crystal begins to increase. This increase in dislocation density leads to a certain congestion in dislocation motion; that is, pileups and tangles of dislocations occur that increase the stress required for continued dislocation motion (and slip) November 24, 2023; 160.

If a cold-worked structure is heated to above six-tenths of the melting point, the dislocation pileups and tangles are rapidly eliminated through increased thermal vibrations of the atoms. This occurs through the processes of recovery and recrystallization. November 23, 2023; 161.

deformation twinning is usually only seen when slip is difficult. November 24, 2023; 162.

Rockwell, Brinell, Vickers, Knoop, and variations within these tests. In general, these tests measure the resistance of the metal to an indenter. November 24, 2023; 163.

## Chapter 12: Drawability and Breaks

Cockcroft and Latham material constant, c, is a fundamental index of workability and drawability. October 12, 2023; 179.

predictor of drawability, ln(A0/Af) November 24, 2023; 179.

In the simplest concept of drawing, a break occurs when the draw stress equals the yield and/or breaking stress of the wire at the die exit November 24, 2023; 185.

During most drawing operations, the surface of the wire undergoes “wear” (wire wear as opposed to die wear), and small pieces of the wire (called “fines”) flake off November 24, 2023; 190.

## Chapter 15: Other Metallurgical Systems for Wire Technology

The resistance of stainless steels to corrosion arises from the tightly adhering, relatively impervious chromium-oxygen layer that forms on the alloy surface. November 24, 2023; 257.